- Introduction

However, wide-bandgap mixed-halide perovskites used in tandem solar cells, which typically exhibit bandgaps of 1.65-1.8 eV, generally suffer from poorer stability than their narrow-bandgap counterparts. The elevated bromide content required to widen the bandgap generally increases deep defect densities, accelerates ion migration and, most critically, induces light- and bias-driven Br/I phase segregation. This compositional demixing results in local bandgap narrowing, photovoltage loss and progressive efficiency degradation during operation [1–3]. Significant progress has been made through compositional engineering, strain management and interfacial passivation[4–6], yet most devices still exhibit sizeable Voc deficits and only partial resistance to prolonged light soaking.

Recent studies increasingly highlight that achieving both high efficiency and long-term stability in WBG perovskites requires controlling not only bulk composition but also crystallization pathways, defect distributions and ion-transport channels within the film[7,8]. In this context, the two step deposition strategy offers distinct advantages over one step routes because it enables more precise control over nucleation and crystal growth. As a result, two step processing can produce dense, vertically oriented, and low defect perovskite films, and has already delivered excellent device performance in narrow bandgap perovskite systems. [9–11]

Generally, two step approaches can be classified into evaporation based and solution-based routes. Although evaporation based two-step deposition provides high uniformity, it typically relies on complex multi-source co evaporation control and high vacuum infrastructure, which increases processing cost and limits manufacturing flexibility. [12] By contrast, fully solution processed two step methods are inherently more compatible with scalable and low-cost coating technologies, such as blade coating, slot die coating and roll to roll manufacturing on industrially relevant substrates. Therefore, solution-based two-step deposition combines the advantages of controllable crystallization kinetics with practical scalability, making it a highly promising platform for fabricating WBG perovskite top cells for monolithic tandem solar modules.

Nevertheless, despite this potential, its application in tandem devices still lags behind that of other fabrication routes. One major limitation is the inefficient and poorly controlled incorporation of bromide into the perovskite lattice, which is crucial for achieving the desired wide bandgap. Introducing bromide via PbBr2 in the first deposition step often promotes the formation of bulky, poorly reactive Pb-Br-rich crystallites, leading to incomplete conversion and substantial residual PbI2 after the second-step reaction[13–15]. Alternatively, supplying Br⁻ predominantly through the second-step organic salts, such as formamidinium bromide or methylammonium bromide, is kinetically constrained by the slow diffusion and exchange of Br⁻ through dense PbI2 or PbCl2-derived matrices [17-19]. As a consequence, films typically suffer from incomplete conversion, vertical halide inhomogeneity and elevated trap densities, which in turn exacerbate light-induced Br/I demixing and accelerate performance degradation.

Analysis

Direct comparison with the GIWAXS patterns of the first-step Pb-halide layers (Fig. 1m,n) elucidate the CsBr-driven phase evolution throughout the conversion process. In the first step films, additional reflections corresponding to CsPb2Br5 are observed, consistent with the formation of a Pb-rich Cs-Pb-Br intermediate embedded within a PbI2-dominated scaffold. After the second-step conversion, nearly all PbI2 is consumed to construct the 3D perovskite framework, while the local chemical environment at grain boundaries becomes relatively Cs-rich rather than Pb-rich. Under these conditions, the thermodynamically favored Cs-Pb-halide derivative shifts from the Pb-rich CsPb2Br5 intermediate toward the Cs-rich region of the phase diagram, resulting in the disappearance of CsPb2Br5 signatures and the emergence of only trace Cs4Pb(Br,I)6in the final perovskite films[16,17].

The underlying interactions between PbI2 and CsBr in the mixed-halide sublattice can be summarized by the following competing reaction pathways

Pb-rich intermediate formation: 2PbI2 + CsBr → CsPb2X5

Cs-rich phase formation: PbI2 + 4CsBr → Cs4PbX6

where X predominantly denotes Br⁻ in the present mixed-halide system.

Overall, the combined SEM and GIWAXS analyses demonstrate that moderate CsBr incorporation around 0.15 M optimally balances scaffold porosity and structural integrity. This balance enables near-complete conversion into a continuous, large-grained, and highly crystalline wide-bandgap perovskite film while simultaneously generating a small amount of electronically benign Cs4Pb(Br,I)6. Insufficient CsBr leads to incomplete conversion and PbI2-rich, defective films, whereas excessive CsBr induces over-porosity, resulting in pinholes and morphological inhomogeneity that compromise film quality and device performance.

Cs4PbBr6 is a zero dimensional perovskite related compound composed of isolated [PbX₆]4- octahedra separated by Cs⁺ ions and exhibits a wide bandgap on the order of 3.5-4.0 eV, with deep valence bands and high lying conduction bands that render it electronically insulating within the spectral region relevant to photocurrent generation[18,19]. When present in trace amounts, this phase preferentially segregates at grain boundaries or surfaces, where it passivates under coordinated Pb and halide sites, reduces trap assisted non radiative recombination and introduces energetic and structural barriers that impede the lateral and vertical migration of halides and vacancies. These effects collectively suppress bromide iodide demixing while leaving charge transport through the three-dimensional perovskite network largely unaffected[20]. Consistent with this picture, Liu et al[21]. demonstrated that spin-coated Cs4PbBr6 nanocrystals on CsPbI2Br films form an interfacial Cs4PbBr6-based layer that lowers trap density and enhances both efficiency and stability; Heo and co-workers[22] employed a spray-coated inorganic 0D Cs4PbBr6 capping layer on CsPbI3 absorbers to improve lattice matching, boost charge extraction and suppress non-radiative recombination; and other studies have introduced Cs4PbBr6 nanocrystals directly into perovskite precursor inks as 0D additives to regulate crystallisation, enrich grain boundaries with a Cs4PbBr6-like phase and improve long-term device stability[20]. However, all these Cs4PbBr6-based passivation schemes rely on pre-synthesised nanocrystals and additional coating and/or annealing steps, often involving organic ligands that must be carefully managed to avoid resistive interlayers. By contrast, our CsBr-assisted two-step route offers a much simpler implementation. The Cs4Pb(Br,I)6-like domains are not introduced as an external additive but form in-situ from the same Pb-halide/CsBr precursor stack via a controlled phase-evolution pathway.

References

[1]	E.T. Hoke, D.J. Slotcavage, E.R. Dohner, A.R. Bowring, H.I. Karunadasa, M.D. McGehee, Reversible photo-induced trap formation in mixed-halide hybrid perovskites for photovoltaics, Chem. Sci. 6 (2014) 613–617. https://doi.org/10.1039/C4SC03141E.

[2]	D.J. Slotcavage, H.I. Karunadasa, M.D. McGehee, Light-Induced Phase Segregation in Halide-Perovskite Absorbers, ACS Energy Lett. 1 (2016) 1199–1205. https://doi.org/10.1021/acsenergylett.6b00495.

[3]	T. Duong, H.K. Mulmudi, Y. Wu, X. Fu, H. Shen, J. Peng, N. Wu, H.T. Nguyen, D. Macdonald, M. Lockrey, T.P. White, K. Weber, K. Catchpole, Light and Electrically Induced Phase Segregation and Its Impact on the Stability of Quadruple Cation High Bandgap Perovskite Solar Cells, ACS Appl. Mater. Interfaces 9 (2017) 26859–26866. https://doi.org/10.1021/acsami.7b06816.

[4]	J. Feng, B. He, Z. Yang, J. Li, M. Zhang, B. Yang, Z. Wu, H. Chen, J. Duan, Q. Tang, Thermal-electrical dual management for efficient and stable wide-bandgap perovskite solar cells, Nano Energy 148 (2026) 111696. https://doi.org/10.1016/j.nanoen.2025.111696.

[5]	X.-Y. He, B. Song, K.-L. Wang, N. Li, L. Huang, R.-H. Qin, J. Chen, C.-H. Chen, Y. Xia, I. Yavuz, Y.-H. Lou, Z.-K. Wang, Stopping Phase Separation Enables Durable Wide-Bandgap Photovoltaic Perovskites, Advanced Materials 38 (2026) e18492. https://doi.org/10.1002/adma.202518492.

[6]	G. Yang, H. Gu, J. Yin, C. Fei, Z. Shi, X. Shi, X. Ying, J. Huang, Reductive cation for scalable wide-bandgap perovskite solar cells in ambient air, Nat Sustain 8 (2025) 456–463. https://doi.org/10.1038/s41893-025-01529-5.

[7]	R. Jiang, Y. Yun, K. Sun, X. Cui, Q. Zhang, C. Hu, C. Jin, Q. Kong, Y. Liu, J. Gong, S. He, L. Qiu, C. Liu, S. Bai, C. Li, Z. Bo, F. Huang, Y.-B. Cheng, T. Bu, Crystallization modulation for wide-bandgap perovskites with universal defect passivation toward efficient perovskite/organic tandem photovoltaics, Nat Commun 17 (2026) 1375. https://doi.org/10.1038/s41467-025-68125-1.

[8]	Y. Xiang, H. Xin, C. Wang, F. Zhou, H. Zhang, P. Hang, L. Xu, X. Yu, J. Xue, D. Yang, Z. Ni, Mechanistic insights into defect-governed ion migration and phase instability in mixed-halide perovskites, Journal of Materials Chemistry A (2026). https://doi.org/10.1039/D5TA10296K.

[9]	M. Wang, Y. Feng, J. Bian, H. Liu, Y. Shi, A comparative study of one-step and two-step approaches for MAPbI3 perovskite layer and its influence on the performance of mesoscopic perovskite solar cell, Chemical Physics Letters 692 (2018) 44–49. https://doi.org/10.1016/j.cplett.2017.12.012.

[10]	A. Ummadisingu, M. Grätzel, Revealing the detailed path of sequential deposition for metal halide perovskite formation, Science Advances 4 (2018) e1701402. https://doi.org/10.1126/sciadv.1701402.

[11]	J. Burschka, N. Pellet, S.-J. Moon, R. Humphry-Baker, P. Gao, M.K. Nazeeruddin, M. Grätzel, Sequential deposition as a route to high-performance perovskite-sensitized solar cells, Nature 499 (2013) 316–319. https://doi.org/10.1038/nature12340.

[12]	T. Abzieher, D. T. Moore, M. Roß, S. Albrecht, J. Silvia, H. Tan, Q. Jeangros, C. Ballif, M. T. Hoerantner, B.-S. Kim, H. J. Bolink, P. Pistor, J. Christoph Goldschmidt, Y.-H. Chiang, S. D. Stranks, J. Borchert, M. D. McGehee, M. Morales-Masis, J. B. Patel, A. Bruno, U. W. Paetzold, Vapor phase deposition of perovskite photovoltaics: short track to commercialization?, (2024). https://doi.org/10.1039/D3EE03273F.

[13]	Inorganic–organic hybrid materials based on PbBr2 and pyridine–hydrazone blocks – structural and theoretical study - RSC Advances (RSC Publishing), (n.d.). https://pubs.rsc.org/en/content/articlelanding/2016/ra/c6ra13462a (accessed September 5, 2025).

[14]	A. Jana, M. Mittal, A. Singla, S. Sapra, Solvent-free, mechanochemical syntheses of bulk trihalide perovskites and their nanoparticles, Chem. Commun. 53 (2017) 3046–3049. https://doi.org/10.1039/C7CC00666G.

[15]	Q. Li, Y. Zhao, W. Zhou, Z. Han, R. Fu, F. Lin, D. Yu, Q. Zhao, Halogen Engineering for Operationally Stable Perovskite Solar Cells via Sequential Deposition, Advanced Energy Materials 9 (2019) 1902239. https://doi.org/10.1002/aenm.201902239.

[16]	Y. Yin, Y. Liu, G. Cao, Z. Lv, H. Zong, Y. Cheng, Q. Dong, C. Liu, M. Li, B. Zhang, Optical properties and mechanical induced phase transition of CsPb2Br5 and CsPbBr3 nanocrystals, Journal of Alloys and Compounds 947 (2023) 169439. https://doi.org/10.1016/j.jallcom.2023.169439.

[17]	J. Li, H. Zhang, S. Wang, D. Long, M. Li, D. Wang, T. Zhang, Inter-Conversion between Different Compounds of Ternary Cs-Pb-Br System, Materials 11 (2018). https://doi.org/10.3390/ma11050717.

[18]	J. Yin, Y. Zhang, A. Bruno, C. Soci, O.M. Bakr, J.-L. Brédas, O.F. Mohammed, Intrinsic Lead Ion Emissions in Zero-Dimensional Cs4PbBr6 Nanocrystals, ACS Energy Lett. 2 (2017) 2805–2811. https://doi.org/10.1021/acsenergylett.7b01026.

[19]	F. Palazon, C. Urso, L. De Trizio, Q. Akkerman, S. Marras, F. Locardi, I. Nelli, M. Ferretti, M. Prato, L. Manna, Postsynthesis Transformation of Insulating Cs4PbBr6 Nanocrystals into Bright Perovskite CsPbBr3 through Physical and Chemical Extraction of CsBr, ACS Energy Lett. 2 (2017) 2445–2448. https://doi.org/10.1021/acsenergylett.7b00842.

[20]	H. Shi, J. Huang, T. Sun, H. Yu, Y. Hu, X. Li, X. Ma, W. Yang, Z. Liu, L. Wang, B. Hu, Y. Shen, M. Wang, Modulating Crystallization of Perovskite Thin Films via Zero-Dimensional Cs4PbBr6 Nanocrystals, Advanced Functional Materials 35 (2025) e08064. https://doi.org/10.1002/adfm.202508064.

[21]	W. Liu, M. Cao, J. Zhang, J. Jiang, H. Yu, X. Hao, J. Zhang, H. Guo, B. Fang, N. Yuan, X. Fan, S. Zhang, J. Ding, Reversible degradation-assisted interface engineering via Cs4PbBr6 nanocrystals to boost the performance of CsPbI2Br perovskite solar cells, Journal of Power Sources 530 (2022) 231294. https://doi.org/10.1016/j.jpowsour.2022.231294.

[22]	J.H. Heo, J.K. Park, H.J. Lee, E.H. Shin, S.Y. Hong, K.-H. Hong, F. Zhang, S.H. Im, Inorganic-Derived 0D Perovskite Induced Surface Lattice Arrangement for Efficient and Stable All-Inorganic Perovskite Solar Cells, Advanced Materials 36 (2024) 2408387. https://doi.org/10.1002/adma.202408387.